## Slide 1
Enhancing Reliability and Quality of Drilled Shafts Through TIP Testing
&
TIP Acceptance Criteria
Matthew Silveston, P.E. Terracon Consultants Inc.
&
George Piscsalko, Pile Dynamics Inc.

## Slide 5
Thermal Integrity Profiling Theory
Slice

## Slide 6
Thermal Integrity Profiling Theory
Cage Shift
1
2
4
3
1
2
4
3

## Slide 7
Thermal Integrity Profiling
Anomaly
1
2
4
3
1
2
4
3
1
4
2

## Slide 8
Thermal Integrity Profiling
Anomaly
1
2
4
3
1
2
4
3

## Slide 9
Thermal Integrity Profiling
Ideal Results

## Slide 10
Thermal Wire
NY/NJ area
Example 1
42” dia with 38” rock socket
27 ft long

## Slide 11
Thermal Wire Setup
Wire 1
Wire 2
Wire 3
Wire 4
North
Example 1

## Slide 12
Thermal Analysis
Example 1
Rock socket
Cage Shift
Soft Bottom
Ambient Soil Temp 55o

## Slide 13
Thermal Analysis
Example 1
Rock socket
Cage Shift
Neck
Cage
Soft Bottom

## Slide 14
Thermal Analysis
NY/NJ Pier 76
Example 1

## Slide 15
Thermal Analysis
Example 1
NY/NJ Pier 76
8,000 psi
1,600 psi

## Slide 16
Thermal Probe
Example 2
Little River
Tallahassee

## Slide 17
Concrete Data
Example 2
36.03 yd3 actual
34.97 yd3 theoretical

## Slide 18
Thermal Probe
Example 2

## Slide 19
Thermal Results
Example 2
Anomaly
Cage Shift
Loose SiSa to hard SiCl
Weathered Limestone
Bottom of Casing

## Slide 20
Thermal Results
Example 2
Anomaly
Cage Shift tubes 2&4

## Slide 21
Thermal Results
Example 2
Anomaly

## Slide 22
Thermal Model of Shaft
Example 2
Osterberg Cell

## Slide 23
CSL vs Thermal
Example 2
Anomaly
Cage Shift
O-cell

## Slide 25: Acceptance Criteria
Load carrying requirements can be controlled by:
  Geotechnical side shear
  Structural bending
  Compression
These are directly related to:
  Circumference surface area of the shaft
  Moment of inertia
  Cross sectional area
Radius Reduction approach will affect each differently:
  Reduction has linear relation to circumference
  Reduction has fourth power relation to moment of inertia
  Reduction has squared relation to area

## Slide 26: Radius Reduction vs. Capacity Reduction

## Slide 27: Cover Loss Considerations on Local Radius Reductions vs. Shaft Diameter
Chart: Shaft Diameter (ft.)
| 3 | 4 | 5 | 6 | 7 | 8 | 9
1.5 inch remaining cover from 6 inch cover | 0.25 | 0.1875 | 0.15 | 0.125 | 0.10714 | 0.09375 | 0.083333
1.5 inch remaining cover from 4 inch cover | 0.13889 | 0.10417 | 0.083333 | 0.069444 | 0.059524 | 0.052083 | 0.046296
1.5 inch remaining cover from 3 inch cover | 0.083333 | 0.0625 | 0.05 | 0.041667 | 0.035714 | 0.03125 | 0.027778
2 inch remaining cover | 0.11111 | 0.083333 | 0.066667 | 0.055556 | 0.047619 | 0.041667 | 0.037037

## Slide 28: Acceptance Criteria
Radius Reduction | Bending Capacity Loss | Compression Capacity Loss | Side Shear Reduction | Cover Loss (4 inch cover, 6ft dia. shaft)
3% | 11% | 6% | 3% | 1.08in
6% | 22% | 12% | 6% | 2.16in
>6% | >22% | >12% | >6% | >2.16in
Satisfactory (S)
0 to 6% Radius Reduction and
Local Cover Criteria Met
Anomaly (A) Requiring further evaluation
Radius Reduction > 6% or
Local Cover Criteria Not Met

## Slide 29
I-5 Bridge over Puyallup River
Tacoma, Washington

## Slide 30: TIP Case History
Wet cast Shaft in Washington State
118” diameter
  10 TIP wires installed
Cage Diameter 102”
126’ shaft length
TIP testing begins immediately after casting
  Data recorded during pour as well as cure
Data recorded for approximately 90 hours after casting
Shaft peak temperature occurs approximately 40 hours after casting
Shaft analysis done at time of one half peak temperature (20 hours)

## Slide 31: TIP Data at Peak Temperature

## Slide 32: TIP Data at time of one half Peak Temperature
Temperature drop is approximately 42 °F between average shaft temperature and local temperature near wires 7, 8, and 9

## Slide 33: TIP Data at one half Peak Temperature

## Slide 34: TIP Results and Acceptance Criteria
Shaft shows a local reduction near wires 6 through 9
  Design radius = 59 inches
  Local effective radius at wires 7 & 8 = 40 inches
  Reduction in Local Radius = 32.2%
    Clearly greater than 6% Reduction in our Criteria
  Cover is also reduced to zero in these regions
    Anomaly extends inside the reinforcing cage
    Below minimum cover requirement
  Shaft fails BOTH the radius reduction criteria AND the cover criteria
  This is considered an anomaly which requires further evaluation
  Coring is done in several locations in the shaft

## Slide 35
4
7
8
9
10
5
6
3
2
1
Coring Locations
Notes: First core was located 18 inches inside the rebar cage and angled towards the cage. Near the depth of the washed out region the core was approximately 6 inches inside the rebar cage.
Zone was hydro-blasted, camera was ran down core holes, and pressure grouting was performed

## Slide 36: Coring Results at approximately 90’ depth
Coring result close to wires 7 and 8, where largest reduction occurred
Coring confirms TIP test results
Zone was hydro-blasted and pressure grouting was performed

## Slide 37: Conclusions
TIP is being used frequently for testing drilled shafts and ACIP piles
TIP can evaluate the area outside the reinforcing cage
An acceptance criteria based upon cover and radius is possible with TIP
The minimum cover specs for a project can be verified
Radius reductions greater than 6% can be easily detected by TIP, alerting the project engineer to further evaluate this anomalous zone

## Slide 38
Thank You