## Slide 1
Dr. Sadik Khan, P.E. (JSU)
Dr. Sahadat Hossain, P.E. (UTA)
Asif Ahmed, (UTA)
Mohammad Faysal (UTA)
EXPANSIVE CLAY PROBLEMS IN TRANSPORTATION GEOTECHNICS: SITE INVESTIGATION, PERFORMANCE MONITORING AND SUSTAINABLE SOLUTIONS

## Slide 2: Expansive Clay in US
Legend:
Red: Clay having high swelling potential
Blue: Less than 50% of clay contents having high swelling potential
Orange: Clay content having slight to moderate swelling potential
Green: Less than 50% of clay contents having slight to moderate swelling potential
Brown: Little or no swelling clay
Yellow: Insufficient data

## Slide 3: Expansive Clay problems in Transportation Geotechnics

## Slide 4: Major Engineering Problems of Expansive Clay
Displacement
Shear Stress
Peak O-C
Fully Softened
Peak N-C
Residual
Chart: Change in Void Ratio
| 1.0 | 3.0 | 5.0
Initial Condition | 0.712 | 0.731 | 0.771
Final Condition | 1.03 | 1.111 | 1.195
Chart: Change in Cohesion
| 0.0 | 1.0 | 3.0 | 5.0
LL = 80 | 0 | 20.4444 | 44.4444 | 53.7778
Chart: Change in Friction Angle
| 0.0 | 1.0 | 3.0 | 5.0
LL = 80 | 0 | 11.8015 | 15.8973 | 20.0972
Decrease in Soil Strength
Slope Failure
EVAPOTRANSPIRATION
PAVEMENTFOUNDATION
WATER CONTENT PROFILE WITH E.T.
HYDROSTATIC WATER CONTENT PROFILE
DRY SEASON
WET SEASON
WATER CONTENT
(COVERED)
ACTIVE ZONE
Volume Change of Soil
Pavement Distress

## Slide 5: Presentation Outline
Instrumentation and performance evaluation of pavement subgrade on expansive soil
Sustainable stabilization of the highway slope failure over expansive soil.

## Slide 6
INSTRUMENTATION AND PERFORMANCE EVALUATION OF PAVEMENT SUBGRADE ON EXPANSIVE SOIL

## Slide 7: Pavement Site for Field Study
SH 342, Ellis County, Dallas, Texas
FM 2757, Kaufman County, Dallas, Texas

## Slide 8: Instrumentation Plan
FM 2757, Kaufman County, Dallas, Texas
SH 342, Ellis County, Dallas, Texas
Moisture and Temperature Sensor
Water Potential Probe

## Slide 9: Field Instrumentation: FM 2757

## Slide 10: Field Instrumentation: SH 342

## Slide 11: Moisture Variation
Chart: Moisture Variation

## Slide 12: Maximum Moisture Variation
June, 13
August, 13
September, 13
October, 13
January, 14
April, 14
Chart: Ground Temperature and Rainfall Variation

## Slide 13
Electrical Resistivity Imaging
Dry Period
Wet Period

## Slide 14: Slab Impulse Response (SIR)
The Slab Impulse Response (Slab IR) method is used to identify and map subgrade voids.
Look for low-stiffness areas associated with hidden damage
  Honeycomb,
  Void
  cracking.
Test Methodology for Slab IR
Surface is impacted with an impulse hammer and the response of the slab is monitored by a geophone placed next to the impact point. The hammer input and the receiver output are recorded.

## Slide 15: SIR Results
Void Index
Flexibility
  Flexibility: Higher values of flexibility indicates less stiffness and poor support condition.
  Void Index Ratio: Peak to mean ratio greater then 4 indicates poor support condition and voids in the pavement section.

## Slide 16
Chart: Inclinometer Profile
| 52.0 | 50.0 | 48.0 | 46.0 | 44.0 | 42.0 | 40.0 | 38.0 | 36.0 | 34.0 | 32.0 | 30.0 | 28.0 | 26.0 | 24.0 | 22.0 | 20.0 | 18.0 | 16.0 | 14.0 | 12.0 | 10.0
14-Mar | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
14-May | 0.5796 | 0.6846 | 0.7938 | 0.627 | 0.4032 | 0.1926 | 0.2406 | 0.3048 | 0.3306 | 0.315 | 0.2832 | 0.3138 | 0.3366 | 0.3372 | 0.3324 | 0.3414 | 0.4182 | 0.642 | 0.7746 | 0.7368 | 0.6162 | 0.468
14-Aug | 0.3306 | 0.9018 | 1.1124 | 0.825 | 0.6702 | 0.8574 | 1.0446 | 1.1754 | 1.176 | 1.2036 | 1.191 | 1.1466 | 1.1532 | 1.1556 | 1.1658 | 1.1334 | 1.2264 | 1.4208 | 1.5354 | 1.4082 | 1.194 | 0.9018
14-Sep | 0.2322 | 0.6882 | 0.9018 | 0.7428 | 0.678 | 1.0818 | 1.3512 | 1.5048 | 1.581 | 1.608 | 1.599 | 1.5486 | 1.5282 | 1.5228 | 1.5366 | 1.4886 | 1.5528 | 1.6266 | 1.623 | 1.4238 | 1.2582 | 0.993
14-Oct | -0.4638 | -0.045 | 0.141 | -0.0852 | -0.222 | 0.1164 | 0.513 | 0.7146 | 0.8352 | 0.855 | 0.867 | 0.7866 | 0.7632 | 0.7578 | 0.777 | 0.708 | 0.7272 | 0.6846 | 0.6156 | 0.4254 | 0.2988 | 0.1812
14-Dec | -0.0222 | 0.1284 | 0.231 | 0.0078 | -0.1632 | 0 | 0.3246 | 0.4872 | 0.549 | 0.5676 | 0.5562 | 0.405 | 0.4404 | 0.4374 | 0.465 | 0.3978 | 0.5178 | 0.6324 | 0.7446 | 0.699 | 0.5886 | 0.4818
15-Jan | 0.6636 | 0.7536 | 0.8094 | 0.5718 | 0.345 | 0.3624 | 0.591 | 0.831 | 0.9666 | 0.9774 | 0.966 | 0.9564 | 0.9426 | 0.9426 | 0.975 | 0.9642 | 1.0728 | 1.236 | 1.3932 | 1.3842 | 1.2936 | 1.1688
15-Feb | 0.5556 | 0.7128 | 0.7896 | 0.4608 | 0.1962 | 0.1524 | 0.336 | 0.5466 | 0.639 | 0.6732 | 0.6564 | 0.6228 | 0.6174 | 0.6192 | 0.6534 | 0.6006 | 0.7602 | 0.9534 | 1.1352 | 1.1376 | 1.044 | 0.8832
15-Mar | 0.2784 | 0.4584 | 0.5598 | 0.2712 | -0.1344 | -0.3684 | -0.2322 | 0.018 | 0.1782 | 0.2496 | 0.249 | 0.126 | 0.1266 | 0.1332 | 0.1788 | 0.1314 | 0.2472 | 0.5202 | 0.768 | 0.783 | 0.6852 | 0.6132
15-Apr | 0.51 | 0.7242 | 0.8322 | 0.5448 | 0.1164 | -0.1392 | 0.051 | 0.2076 | 0.267 | 0.2838 | 0.2658 | 0.246 | 0.2184 | 0.2226 | 0.2706 | 0.222 | 0.3744 | 0.6564 | 0.8976 | 0.927 | 0.8268 | 0.6522
15-May | 0.6012 | 0.7218 | 0.861 | 0.6126 | 0.1524 | -0.1542 | -0.0906 | 0.1518 | 0.2886 | 0.321 | 0.3042 | 0.204 | 0.2376 | 0.2442 | 0.3024 | 0.2538 | 0.4692 | 0.6942 | 0.9726 | 1.0074 | 0.9264 | 0.8058
15-Jun | 0.7206 | 0.8496 | 1.0044 | 0.771 | 0.318 | -0.045 | 0.1512 | 0.4128 | 0.5028 | 0.5334 | 0.5292 | 0.447 | 0.4398 | 0.447 | 0.507 | 0.4362 | 0.6102 | 0.8916 | 1.1622 | 1.1862 | 1.1016 | 1.0284
Horizontal Inclinometer Profile

## Slide 17
SUSTAINABLE STABILIZATION OF THE HIGHWAY SLOPES FAILURE OVER EXPANSIVE SOIL

## Slide 18: Slope Movement Investigation
Resistivity Profile: RI-1
Resistivity Profile: RI-2
Chart: Plasticity Chart
| 50.0 | 60.0 | 72.0 | 64.0
BH-1 | 25 | 33 | 48 | 38
BH-2 | 26 | 38 | 45 | 35 | 37
BH-3 | 27 | 34 | 51 | 32
A Line | 0 | 7.3 | 14.6 | 21.9 | 29.2 | 36.5 | 43.8 | 51.1 | 58.4
U-Line | 10.8 | 19.8 | 28.8 | 37.8 | 46.8 | 55.8 | 64.8 | 73.8 | 82.8
LL-50 | 0 | 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80
Displacement
Shear Stress
Peak O-C
Fully Softened
Peak N-C
Residual

## Slide 19: Recycled Plastic Pin to Stabilize Shallow Slope Failure
Recycled Plastic Pin (RPP)
  Mainly Polymeric Materials
  Fabricated from Recycled Plastics
  Commercially Available
  RPP Reduces Waste Volume
  Resistant to Biological Exposure
A 10’ long RPP can replace 500 Soda Bottles
  50 Billion Water Bottle end up in US Landfill Each Year
  It takes 700 year to decompose plastic bottles
  Ecosystems and wildlife are negatively impacted by plastic debris.

## Slide 20: Design of Slope Stabilization
Reinforced Section 1: FS = 1.43
Reinforced Section 2: FS = 1.48
Reinforced Section 3: FS = 1.54
Soil Type | Friction Angle | Cohesion | Unit Weight | Elastic Modulus
 | φ | c | ϒ | E
- | ◦ | psf | pcf | psf
1 | 10 | 100 | 125 | 100000
2 | 23 | 100 | 125 | 150000
3 | 15 | 250 | 130 | 200000
4 | 35 | 3000 | 140 | 250000
Back Analysis of Unreinforced Slope: FS = 1.05
Soil 4
Soil 3
Soil 2
Soil 1
Back Calculated Soil Parameters

## Slide 21: RPP Layout

## Slide 22: Installation of RPP
Equipment: Klemm 802 Drill Rig
Hammer Type: KD 1101

## Slide 23: Instrumentation of the Slope
Rain Gauge
Instrumented RPP
Surveying
Inclinometer
Moisture Sensor
Water Potential Probe

## Slide 24: Settlement at Crest
Chart: Total Settlement of at the crest of US 287 slope
| 0.0 | 6.08768 | 17.53192800000024 | 23.435928 | 29.15690400000024 | 34.73257600000051 | 40.73005600000001 | 45.942632 | 51.49993600000001 | 57.267488 | 63.30596800000001 | 69.17979199999817 | 75.00540000000001 | 81.27249599999988 | 87.15812799999995 | 92.95388799999998 | 98.758504 | 104.48604 | 110.26704 | 115.901096 | 121.647328 | 127.3758479999977 | 133.274599999994 | 138.987704 | 157.0188480000005 | 161.7236799999999 | 165.681656 | 170.2707039999941 | 175.076888 | 179.539984 | 184.6990959999993 | 188.685936 | 193.5160639999997 | 197.9086400000005 | 202.80896 | 207.417032 | 212.11432 | 217.3918400000025 | 222.0097519999938 | 226.899904 | 231.6254 | 236.514895999994 | 241.2131679999942 | 245.471264
5.6.12 | 0.84646 | 1.9134 | 1.1614 | 2.126 | 2.189 | 1.5276 | 2.8071 | 4.2756 | 4.5039 | 7.3425 | 14.6063 | 14.2087 | 6.0866 | 5.7323 | 4.4921 | 3.0472 | 3.063 | 2.0394 | 2.3898 | 3.4409 | 4.6929 | 4.815 | 2.7874 | 3.1535 | 1.5551 | 2.2992 | 5.7717 | 8.0591 | 6.6024 | 6.2795 | 5.6457 | 2.6772 | 2.7874 | 3.9094 | 3.9921 | 4.1575 | 3.063 | 3.4764 | 2.4843 | 2.815 | 3.5197 | 3.8465 | 3.0157 | 1.7677
5.6.12 | 0.84646 | 1.9134 | 1.1614 | 2.126 | 2.189 | 1.5276 | 2.8071 | 4.2756 | 4.5039 | 7.3425 | 14.6063 | 14.2087 | 6.0866 | 5.7323 | 4.4921 | 3.0472 | 3.063 | 2.0394 | 2.3898 | 3.4409 | 4.6929 | 4.815 | 2.7874 | 3.1535 | 1.5551 | 2.2992 | 5.7717 | 8.0591 | 6.6024 | 6.2795 | 5.6457 | 2.6772 | 2.7874 | 3.9094 | 3.9921 | 4.1575 | 3.063 | 3.4764 | 2.4843 | 2.815 | 3.5197 | 3.8465 | 3.0157 | 1.7677
6.6.12 | 0.27953 | 1.5512 | 1.5394 | 1.8976 | 2.2992 | 1.126 | 1.7717 | 4.6024 | 4.6772 | 8.2598 | 14.1575 | 13.9173 | 6.2992 | 6.0354 | 4.7283 | 3.4961 | 2.3307 | 1.6299 | 1.9803 | 3.6417 | 5.3425 | 4.6811 | 2.4764 | 3.1299 | 1.5551 | 2.3819 | 6.4921 | 7.9409 | 7.4764 | 6.6063 | 6.0079 | 3.3504 | 2.5197 | 4.0315 | 4.1102 | 3.9055 | 3.4213 | 3.5354 | 2.3937 | 2.9803 | 3.4764 | 4.6575 | 3.7087 | 2.6535
7.13.12 | 0.7126 | 1.4803 | 1.6063 | 1.9409 | 2.1614 | 1.4016 | 1.3976 | 3.9882 | 5.6575 | 6.7677 | 11.5512 | 15.5157 | 6.3583 | 6.311 | 5.0866 | 3.9528 | 3.6063 | 2.252 | 2.3819 | 3.5866 | 4.9724 | 5.2953 | 2.9567 | 2.8386 | 1.5984 | 2.563 | 6.4685 | 7.9252 | 7.437 | 7.0118 | 6.3937 | 3.6417 | 2.9449 | 4.2244 | 4.1181 | 4.1417 | 3.6732 | 2.8543 | 2.9843 | 3.0906 | 3.374 | 5.0945 | 4.248 | 2.7953
8.3.12 | 0 | 1.4331 | 1.7992 | 2.5906 | 1.9764 | 1.7992 | 2.1417 | 4.437 | 5.3268 | 5.437 | 11.4016 | 16.0984 | 5.8268 | 6.6181 | 5.6378 | 3.563 | 3.5669 | 2.1575 | 2.752 | 3.878 | 4.5236 | 4.7205 | 2.8268 | 3.0591 | 1.9606 | 2.4843 | 6.4173 | 8.2047 | 7.9409 | 6.6417 | 6.1417 | 3.2402 | 3.122 | 3.7087 | 3.7598 | 3.5551 | 3.437 | 3.0315 | 2.7559 | 3.1417 | 3.7559 | 4.2795 | 3.9094 | 2.2047
9.8.12 | 0.63386 | 2.0433 | 1.3425 | 2.3504 | 2.2165 | 1.5118 | 2.3307 | 4.5472 | 5.252 | 5.5433 | 12.9843 | 15.4331 | 6.063 | 6.5591 | 5.8346 | 3.9882 | 3.6457 | 2.811 | 2.7992 | 4.2874 | 4.9961 | 5.185 | 3.2638 | 3.4606 | 1.8307 | 2.5276 | 6.4724 | 8.6142 | 8.5197 | 7.1339 | 6.0039 | 3.2165 | 3.4764 | 4.1378 | 3.7244 | 3.5787 | 3.5866 | 3.1339 | 2.9921 | 3.122 | 3.3504 | 4.2795 | 3.9094 | 2.2047
10.6.12 | 0.80315 | 2.3976 | 1.5472 | 2.2087 | 2.2559 | 2.0827 | 2.1181 | 4.4685 | 4.7323 | 8.2677 | 12.2047 | 14.9606 | 6.185 | 6.5039 | 5.4685 | 3.8031 | 3.5472 | 2.4488 | 2.6142 | 3.9646 | 5.0157 | 4.8976 | 3.4173 | 3.5197 | 1.6063 | 2.5276 | 5.3543 | 8.6811 | 8.2165 | 7.1457 | 6.3661 | 3.4055 | 3.1496 | 4.126 | 4.1969 | 4.0276 | 3.5709 | 3.0276 | 3.1378 | 3.3268 | 3.8661 | 4.2795 | 3.9094 | 2.2047
11.10.12 | 0.7874 | 2.2244 | 1.2559 | 2.1732 | 1.9134 | 2.1772 | 1.9961 | 4.5709 | 5.1024 | 9.1772 | 12.1732 | 15.0512 | 6.3228 | 6.9685 | 5.185 | 3.7441 | 3.4961 | 3.0276 | 2.7244 | 4.315 | 5.1102 | 4.752 | 3.1181 | 3.4094 | 1.5472 | 2.2992 | 6.3425 | 8.5197 | 8.2283 | 7.1024 | 6.5039 | 3.126 | 2.9567 | 4.248 | 4.1457 | 4.3228 | 3.5827 | 3.0591 | 2.9606 | 3.9803 | 3.2283 | 4.2795 | 3.9094 | 2.2047
12.13.12 | 0.80315 | 2.3976 | 1.5472 | 2.2087 | 2.2717 | 1.815 | 2.0866 | 4.689 | 5.1969 | 7.6102 | 12.2047 | 14.9606 | 6.0315 | 6.9291 | 5.5118 | 3.626 | 3.9803 | 3.0709 | 3.0394 | 4.1693 | 5.4764 | 5.1535 | 3.1535 | 3.7087 | 2.0236 | 2.4134 | 6.063 | 8.311 | 8.311 | 7.1732 | 6.1417 | 3.3661 | 3.185 | 4.1772 | 4.3701 | 4.2323 | 3.2598 | 3.0591 | 2.9606 | 3.9803 | 3.2283 | 4.2795 | 3.9094 | 2.2047
1.10.13 | 0.7874 | 2.1063 | 1.5551 | 2.0709 | 2.1181 | 1.8386 | 2.0079 | 4.3307 | 4.4764 | 4.3031 | 12.2677 | 13.9449 | 6.1654 | 6.5472 | 5.2126 | 3.8307 | 3.6417 | 2.5315 | 2.6181 | 3.9291 | 4.7913 | 4.8661 | 3.1457 | 3.4724 | 1.7953 | 2.3583 | 6.248 | 8.6575 | 8.2756 | 6.7244 | 6.6063 | 3.311 | 3.0157 | 4.378 | 4.063 | 3.9606 | 3.2756 | 3.2638 | 2.9606 | 3.9803 | 3.2283 | 4.2795 | 3.9094 | 2.2047
2.9.13 | 1.0394 | 2.4213 | 2 | 1.3858 | 1.9961 | 1.8465 | 1.8858 | 4.9252 | 4.3937 | 4.122 | 11.878 | 13.9843 | 5.748 | 6.6457 | 5.4016 | 3.7441 | 3.7913 | 2.6181 | 2.378 | 4.4016 | 4.4291 | 4.5354 | 3 | 2.189 | 1.8937 | 2.1929 | 6.4331 | 8.4488 | 8.9291 | 6.6378 | 4.9094 | 3.1496 | 3.1654 | 4.2165 | 4.3937 | 4.0118 | 3.748 | 3.6575 | 2.9606 | 3.9803 | 3.2283 | 4.2795 | 3.9094 | 2.2047
3.7.13 | 2.0118 | 2.378 | 1.3622 | 2.2953 | 2.0748 | 2.1457 | 1.8189 | 4.4803 | 5.0906 | 5.185 | 11.4843 | 14.1732 | 5.8819 | 6.3583 | 5.0354 | 3.3346 | 4.7717 | 2.8425 | 2.7126 | 4.0315 | 4.4606 | 5.063 | 2.8386 | 3.6378 | 1.0945 | 2.5472 | 5.7756 | 8.9213 | 8.1496 | 6.8504 | 6.0354 | 3.1929 | 2.8307 | 3.5276 | 3.9567 | 3.3228 | 3.6339 | 3.6614 | 2.9528 | 3.9803 | 3.2283 | 4.2795 | 3.9094 | 2.2047

## Slide 25: Horizontal Movement
Chart: Comparison of Horzontal Movement at US 287 Slope
2.5 ft-Inc1 | -0.0198 | 0.0846 | 0.2688 | 0.447 | 0.6492 | 0.3666 | 0.3882 | 0.1998 | 0.078 | 0.0474 | -0.1422 | -0.1398 | -0.0288 | -0.036 | 0.2976 | 0.3198 | 0.2682 | 0.4896 | 0.6486 | 1.0458 | 1.0584 | 1.032 | 1.1868 | 1.443 | 1.2306 | 1.203 | 1.2012 | 1.182 | 1.0026 | 1.4262 | 1.0584 | 1.1988 | 1.236 | 1.2054 | 1.3296 | 1.3062 | 1.0176
2.5 ft-Inc 3 | 0.06 | 0.0084 | 0.2616 | 0.2154 | 0.4638 | 0.459 | 0.5064 | 0.468 | 0.4572 | 0.345 | 0.2454 | 0.2514 | 0.4104 | 0.4026 | 0.7086 | 0.7764 | 0.732 | 0.9228 | 1.0548 | 1.3014 | 1.3704 | 1.299 | 1.3506 | 1.5498 | 1.4904 | 1.5222 | 1.5036 | 1.5192 | 1.4688 | 1.5516 | 1.6476 | 1.6722 | 1.5876 | 1.7808 | 1.8822 | 1.8654 | 1.8072

## Slide 26: Comparison of Rainfall, Moisture Content, Matric Suction and Hor. Displacement
Chart: Moisture Content (%)
Chart: Matric Suction (psf)
Chart: Date
| 40749.0 | 40763.0 | 40784.0 | 40799.0 | 40814.0 | 40837.0 | 40858.0 | 40890.0 | 40912.0 | 40921.0 | 40943.0 | 40965.0 | 40983.0 | 41007.0 | 41031.0 | 41054.0 | 41079.0 | 41095.0 | 41124.0 | 41163.0 | 41177.0 | 41194.0 | 41205.0 | 41233.0 | 41256.0 | 41278.0 | 41284.0 | 41297.0 | 41314.0 | 41328.0 | 41352.0 | 41369.0 | 41389.0 | 41414.0 | 41435.0 | 41456.0 | 41488.0
2.5 ft-Inc1 | -0.0198 | 0.0846 | 0.2688 | 0.447 | 0.6492 | 0.3666 | 0.3882 | 0.1998 | 0.078 | 0.0474 | -0.1422 | -0.1398 | -0.0288 | -0.036 | 0.2976 | 0.3198 | 0.2682 | 0.4896 | 0.6486 | 1.0458 | 1.0584 | 1.032 | 1.1868 | 1.443 | 1.2306 | 1.203 | 1.2012 | 1.182 | 1.0026 | 1.4262 | 1.0584 | 1.1988 | 1.236 | 1.2054 | 1.3296 | 1.3062 | 1.0176
6.5 ft-Inc 1 | -0.0258 | 0.036 | 0.1752 | 0.321 | 0.501 | 0.3588 | 0.3288 | 0.2862 | 0.216 | 0.1674 | -0.039 | -0.0504 | -0.0132 | -0.0942 | 0.1308 | 0.138 | 0.099 | 0.2634 | 0.4476 | 0.7902 | 0.7956 | 0.8112 | 0.9348 | 1.1286 | 0.9408 | 0.9294 | 0.9834 | 0.99 | 0.8484 | 1.0902 | 0.9078 | 0.9504 | 0.978 | 0.948 | 1.0116 | 0.999 | 0.8376
10.5 ft-Inc 1 | -0.0246 | -0.003 | 0.0726 | 0.1728 | 0.3048 | 0.1836 | 0.1632 | 0.1644 | 0.1644 | 0.1602 | 0.0432 | 0.0606 | 0.081 | 0.0024 | 0.1224 | 0.1254 | 0.063 | 0.1446 | 0.246 | 0.4296 | 0.4128 | 0.4326 | 0.5322 | 0.6522 | 0.5214 | 0.5262 | 0.5964 | 0.591 | 0.4896 | 0.6924 | 0.549 | 0.6 | 0.6276 | 0.6228 | 0.6102 | 0.6114 | 0.4452
20.5 ft-Inc 1 | -0.0192 | -0.0246 | -0.006 | 0.0372 | 0.0948 | 0.0132 | -0.0072 | -0.0018 | 0.0108 | 0.0228 | -0.0066 | 0.0156 | 0.0276 | 0.015 | 0.0498 | 0.051 | 0.0246 | 0.0552 | 0.0642 | 0.105 | 0.0768 | 0.0768 | 0.1056 | 0.159 | 0.078 | 0.0786 | 0.1074 | 0.1074 | 0.0498 | 0.174 | 0.081 | 0.1152 | 0.135 | 0.1308 | 0.1368 | 0.1338 | 0.0882
Rainfall
M/C
Matric Suction
Displacement
Chart: Rainfall (inch)
Average Rainfall | 2.27 | 3.05 | 3.84 | 3.34 | 3.99 | 4.12 | 2.66 | 2.34 | 3.05 | 4.45 | 3.03 | 3.1 | 2.27 | 3.05 | 3.84 | 3.34 | 3.99 | 4.12 | 2.66 | 2.34 | 3.05 | 4.45 | 3.03 | 3.1 | 2.27 | 3.05 | 3.84 | 3.34 | 3.99 | 4.12 | 2.66 | 2.34
Total Rainfall | 2.089 | 0.59961 | 0 | 4.4799 | 3.3228 | 0.94882 | 0.011811 | 0.12992 | 1.5198 | 3.2456 | 2.0079 | 5.5984 | 7.8819 | 3.315 | 6.1339 | 0.73921 | 4.85 | 3.49 | 3.18 | 2.18 | 3.31 | 0.87 | 0.18 | 2.13 | 3.3819 | 1.8 | 1.87 | 2.49 | 4.31 | 2.51 | 3.603 | 0.27

## Slide 27: Expansive Behavior
Chart: Comparison of Horizontal Movement with Temperature
2.5 ft-Inc1 | -0.0198 | 0.0846 | 0.2688 | 0.447 | 0.6492 | 0.3666 | 0.3882 | 0.1998 | 0.078 | 0.0474 | -0.1422 | -0.1398 | -0.0288 | -0.036 | 0.2976 | 0.3198 | 0.2682 | 0.4896 | 0.6486 | 1.0458 | 1.0584 | 1.032 | 1.1868 | 1.443 | 1.2306 | 1.203 | 1.2012 | 1.182 | 1.0026 | 1.4262 | 1.0584 | 1.1988 | 1.236 | 1.2054 | 1.3296 | 1.3062 | 1.0176
2.5 ft-Inc 3 | 0.06 | 0.0084 | 0.2616 | 0.2154 | 0.4638 | 0.459 | 0.5064 | 0.468 | 0.4572 | 0.345 | 0.2454 | 0.2514 | 0.4104 | 0.4026 | 0.7086 | 0.7764 | 0.732 | 0.9228 | 1.0548 | 1.3014 | 1.3704 | 1.299 | 1.3506 | 1.5498 | 1.4904 | 1.5222 | 1.5036 | 1.5192 | 1.4688 | 1.5516 | 1.6476 | 1.6722 | 1.5876 | 1.7808 | 1.8822 | 1.8654 | 1.8072
Desiccation Crack
(Dry Period)
No Cracks
(Wet Period)

## Slide 28: Settlement at Control Section
R. Section 1
Control Section
Control Section 2
R. Section 3
Settlement: 15 in
Settlement: 9 in

## Slide 29: Comparison of Performance Northbound and Southbound (Reinforced) Slope
Failure Location 3
Failure Location 4
Failure Location | Time
Failure Location-1 | October 2013
Failure Location -2 | October 2013
Failure Location-3 | June 2015
Failure Location-4 | June 2015
Failure Location 1
Failure Location 2
Failure Location 3

## Slide 30: Failure of Northbound Slope After Repair
Chart: Date
Slope Failed on 1st week of November , 2015

## Slide 31
Thank You